## Slide 1: Chapter 5: Diffusion
ISSUES TO ADDRESS...
• How does diffusion occur?
• Why is it an important part of processing?
• How can the rate of diffusion be predicted for
some simple cases?
• How does diffusion depend on structure
and temperature?

## Slide 2: Diffusion
Diffusion - Mass transport by atomic motion
Mechanisms
Gases & Liquids – random (Brownian) motion
Solids – vacancy diffusion or interstitial diffusion

## Slide 3: Diffusion
• Interdiffusion: In an alloy, atoms tend to migrate
from regions of high conc. to regions of low conc.
Initially
Figs. 5.1 & 5.2, Callister & Rethwisch 9e.
After some time

## Slide 4: Diffusion
• Self-diffusion: In an elemental solid, atoms
also migrate.
Label some atoms
A
B
C
D
After some time
A
B
C
D

## Slide 5: Diffusion Mechanisms
Vacancy Diffusion:
• atoms exchange with vacancies
• applies to substitutional impurities atoms
• rate depends on:
-- number of vacancies
-- activation energy to exchange.
increasing elapsed time

## Slide 6: Diffusion Simulation
• Simulation of
interdiffusion
across an interface:
• Rate of substitutional
diffusion depends on:
-- vacancy concentration
-- frequency of jumping
(Courtesy P.M. Anderson)
This slide contains an animation that requires Quicktime and a Cinepak decompressor. Click on the message or image below to activate the animation.

## Slide 7: Diffusion Mechanisms
Interstitial diffusion – smaller atoms can diffuse between atoms.
More rapid than vacancy diffusion
Fig. 5.3 (b), Callister & Rethwisch 9e.

## Slide 8: Processing Using Diffusion
Chapter-opening photograph, Chapter 5, Callister & Rethwisch 9e. (Courtesy of
Surface Division, Midland-Ross.)
• Case Hardening:
-- Diffuse carbon atoms
into the host iron atoms
at the surface.
-- Example of interstitial
diffusion is a case
hardened gear.
• Result: The presence of C atoms makes iron (steel) harder.

## Slide 9: Processing Using Diffusion
• Doping silicon with phosphorus for n-type semiconductors:
• Process:
3. Result: Doped
semiconductor
regions.
silicon
magnified image of a computer chip
0.5 mm
light regions: Si atoms
light regions: Al atoms
2. Heat it.
1. Deposit P rich
layers on surface.
silicon
Adapted from Figure 18.27, Callister & Rethwisch 9e.

## Slide 10: Diffusion
How do we quantify the amount or rate of diffusion?
J  slope
M =
mass
diffused
time
Measured empirically
  Make thin film (membrane) of known cross-sectional area
  Impose concentration gradient
  Measure how fast atoms or molecules diffuse through the membrane

## Slide 11: Steady-State Diffusion
Fick’s first law of diffusion
C1
C2
x
C1
C2
x1
x2
D  diffusion coefficient
Rate of diffusion independent of time
  Flux proportional to concentration gradient =

## Slide 12: Example: Chemical Protective Clothing (CPC)
Methylene chloride is a common ingredient of paint removers. Besides being an irritant, it also may be absorbed through skin. When using this paint remover, protective gloves should be worn.
If butyl rubber gloves (0.04 cm thick) are used, what is the diffusive flux of methylene chloride through the glove?
Data:
  diffusion coefficient in butyl rubber: D = 110 x10-8 cm2/s
  surface concentrations:
C2 = 0.02 g/cm3
C1 = 0.44 g/cm3

## Slide 13: Example (cont).
glove
C1
C2
skin
paint
remover
x1
x2
Solution – assuming linear conc. gradient
x2 – x1 = 0.04 cm
Data:
C1 = 0.44 g/cm3
C2 = 0.02 g/cm3
D = 110 x 10-8 cm2/s

## Slide 14: Diffusion and Temperature
• Diffusion coefficient increases with increasing T
D
=
Do
exp
-
Qd
R
T
= pre-exponential [m2/s]
= diffusion coefficient [m2/s]
= activation energy [J/mol or eV/atom]
= gas constant [8.314 J/mol-K]
= absolute temperature [K]
D
Do
Qd
R
T

## Slide 15: Diffusion and Temperature
Adapted from Fig. 5.7, Callister & Rethwisch 9e. (Data for Fig. 5.7 taken from E.A. Brandes and G.B. Brook (Ed.) Smithells Metals Reference Book, 7th ed., Butterworth-Heinemann, Oxford, 1992.)
D has exponential dependence on T
D
interstitial
>> D
substitutional
C in α-Fe
C in γ-Fe
Al in Al
Fe in α-Fe
Fe in γ-Fe
1000 K/T
D (m2/s)
C in α-Fe
C in g-Fe
Al in Al
Fe in α-Fe
Fe in γ-Fe
0.5
1.0
1.5
10-20
10-14
10-8
T(°C)
1500
1000
600
300

## Slide 16
Example: At 300°C the diffusion coefficient and activation energy for Cu in Si are
D(300°C) = 7.8 x 10-11 m2/s
Qd = 41.5 kJ/mol
What is the diffusion coefficient at 350°C?
transform data
D
Temp = T
ln D
1/T

## Slide 17: Example (cont.)
T1 = 273 + 300 = 573 K
T2 = 273 + 350 = 623 K
D2 = 15.7 x 10-11 m2/s

## Slide 18: Non-steady State Diffusion
The concentration of diffusing species is a function of both time and position C = C(x,t)
In this case Fick’s Second Law is used
Fick’s Second Law
Notes: In the non-steady state the concentration profile develops with time.

## Slide 19: VMSE: Screenshot of Diffusion Computations & Data Plots

## Slide 20: Non-steady State Diffusion
Fig. 5.5, Callister & Rethwisch 9e.
B.C. at t = 0, C = Co for 0  x  ∞
at t > 0, C = CS for x = 0 (constant surface conc.)
C = Co for x = ∞
• Copper diffuses into a bar of aluminum.
pre-existing conc., Co of copper atoms
Surface conc.,
C
of Cu atoms
bar
s
C
s

## Slide 21: Solution:
C(x,t) = Conc. at point x at time t
erf(z) = error function
erf(z) values are given in Table 5.1
CS
Co
C(x,t)
Fig. 5.5, Callister & Rethwisch 9e.

## Slide 22: Non-steady State Diffusion
Sample Problem: An FCC iron-carbon alloy initially containing 0.20 wt% C is carburized at an elevated temperature and in an atmosphere that gives a surface carbon concentration constant at 1.0 wt%. If after 49.5 h the concentration of carbon is 0.35 wt% at a position 4.0 mm below the surface, determine the temperature at which the treatment was carried out.
Solution: use Eqn. 5.5

## Slide 23: Solution (cont.):
  t = 49.5 h x = 4 x 10-3 m
  Cx = 0.35 wt% Cs = 1.0 wt%
  Co = 0.20 wt%
 erf(z) = 0.8125

## Slide 24: Solution (cont.):
We must now determine from Table 5.1 the value of z for which the error function is 0.8125. An interpolation is necessary as follows
z
erf(z)
0.90 0.7970
z 0.8125
0.95 0.8209
z = 0.93
Now solve for D

## Slide 25
To solve for the temperature at which D has the above value, we use a rearranged form of Equation (6.9a);
from Table 6.2, for diffusion of C in FCC Fe
Do = 2.3 x 10-5 m2/s Qd = 148,000 J/mol

Solution (cont.):
T = 1300 K = 1027°C

## Slide 26: Example: Chemical Protective Clothing (CPC)
Methylene chloride is a common ingredient of paint removers. Besides being an irritant, it also may be absorbed through skin. When using this paint remover, protective gloves should be worn.
If butyl rubber gloves (0.04 cm thick) are used, what is the breakthrough time (tb), i.e., how long could the gloves be used before methylene chloride reaches the hand?
Data
  diffusion coefficient in butyl rubber:
  D = 110 x 10-8 cm2/s

## Slide 27: CPC Example (cont.)
Time required for breakthrough ca. 4 min
glove
C1
C2
skin
paint
remover
x1
x2
Solution – assuming linear conc. gradient
Equation from online CPC Case Study 5 at the Student Companion Site for Callister & Rethwisch 9e (www.wiley.com/
college/callister)
D = 110 x 10-8 cm2/s
Breakthrough time = tb

## Slide 28: Summary
Diffusion FASTER for...
• open crystal structures
• materials w/secondary
bonding
• smaller diffusing atoms
• lower density materials
Diffusion SLOWER for...
• close-packed structures
• materials w/covalent
bonding
• larger diffusing atoms
• higher density materials