## Slide 1: Chapter 4: Imperfections in Solids
ISSUES TO ADDRESS...
• What types of defects arise in solids?
• Can the number and type of defects be varied
and controlled?
• How do defects affect material properties?
• Are defects undesirable?
• What are the solidification mechanisms?

## Slide 2: Imperfections in Solids
Solidification- result of casting of molten material
  2 steps
    Nuclei form
    Nuclei grow to form crystals – grain structure
Start with a molten material – all liquid
Crystals grow until they meet each other
Adapted from Fig. 4.15 (b), Callister & Rethwisch 9e.
grain structure
crystals growing
nuclei
liquid
[Photomicrograph courtesy of L. C. Smith and C. Brady, the National Bureau of Standards, Washington, DC (now the National Institute of Standards and Technology, Gaithersburg, MD.)]

## Slide 3: Polycrystalline Materials
Grain Boundaries
regions between crystals
transition from lattice of one region to that of the other
slightly disordered
low density in grain boundaries
  high mobility
  high diffusivity
  high chemical reactivity
Adapted from Fig. 4.8, Callister & Rethwisch 9e.

## Slide 4: Solidification
Columnar in area with less undercooling
Shell of equiaxed grains due to rapid cooling (greater ΔT) near wall
Grain Refiner - added to make smaller, more uniform, equiaxed grains.
heat
flow
Adapted from Fig. 5.17, Callister & Rethwisch 3e. (Reproduced with permission from Metals Handbook, Vol. 9, 9th edition, Metallography and Microstructures, ASM International, Materials Park,
OH, 1985.)
~ 8 cm
Grains can be - equiaxed (roughly same size in all directions)
  - columnar (elongated grains)

## Slide 5: Imperfections in Solids
There is no such thing as a perfect crystal.
What are these imperfections?
Why are they important?
Many of the important properties of materials are due to the presence of imperfections.

## Slide 6: Types of Imperfections
• Vacancy atoms
• Interstitial atoms
• Substitutional atoms
Point defects
• Dislocations
Line defects
• Grain Boundaries
Area defects

## Slide 7: Point Defects in Metals
• Vacancies:
-vacant atomic sites in a structure.
• Self-Interstitials:
-"extra" atoms positioned between atomic sites.
Vacancy
distortion
of planes
self-
interstitial
distortion
of planes

## Slide 8: Equilibrium Concentration: Point Defects
Boltzmann's constant
(1.38 x 10
-23
J/atom-K)
(8.62
x
10
-5
eV/atom-K)
N
v
N
=
exp

Q
v
k
T
No. of defects
No. of potential
defect sites
Activation energy
Temperature
Each lattice site
is a potential
vacancy site
• Equilibrium concentration varies with temperature!

## Slide 9: Measuring Activation Energy
• We can get Qv from
an experiment.
N
v
N
=
exp
-
Q
v
k
T
• Measure this...
N
v
N
T
exponential
dependence!
defect concentration
• Replot it...
1/
T
N
N
v
ln
-
Q
v
/k
slope

## Slide 10: Estimating Vacancy Concentration
• Find the equil. # of vacancies in 1 m3 of Cu at 1000C.
• Given:
A
Cu
= 63.5 g/mol
ρ
= 8.4 g
/
cm
3
Q
v
= 0.9 eV/atom
N
A
= 6.02 x 1023
atoms/mol
For 1 m3
, N =
N
A
A
Cu
ρ
x
x
1 m3
= 8.0 x 1028 sites
• Answer:
N
v
=
(2.7 x 10-4)(8.0 x 1028) sites = 2.2 x 1025 vacancies
= 2.7 x 10-4
8.62 x 10-5
eV/atom-K
0.9 eV/atom
1273 K
N
v
N
=
exp
-
Q
v
k
T

## Slide 11: Observing Equilibrium Vacancy Conc.
• Low energy electron
microscope view of
a (110) surface of NiAl.
• Increasing temperature causes surface island of
atoms to grow.
• Why? The equil. vacancy
conc. increases via atom
motion from the crystal
to the surface, where
they join the island.
Reprinted with permission from Nature (K.F. McCarty, J.A. Nobel, and N.C. Bartelt, "Vacancies in
Solids and the Stability of Surface Morphology",
Nature, Vol. 412, pp. 622-625 (2001). Image is
5.75 mm by 5.75 mm.) Copyright (2001) Macmillan Publishers, Ltd.
I
sland grows/shrinks to maintain
equil. vancancy conc. in the bulk.

## Slide 12: Imperfections in Metals (i)
Two outcomes if impurity (B) added to host (A):
• Solid solution of B in A (i.e., random dist. of point defects)
• Solid solution of B in A plus particles of a new
phase (usually for a larger amount of B)
OR
Substitutional solid soln.
(e.g., Cu in Ni)
Interstitial solid soln.
(e.g., C in Fe)
Second phase particle
-- different composition
-- often different structure.

## Slide 13: Imperfections in Metals (ii)
Conditions for substitutional solid solution (S.S.)
W. Hume – Rothery rule
  1. Δr (atomic radius) < 15%
  2. Proximity in periodic table
    i.e., similar electronegativities
  3. Same crystal structure for pure metals
  4. Valency
    All else being equal, a metal will have a greater tendency to dissolve a metal of higher valency than one of lower valency

## Slide 14: Imperfections in Metals (iii)
Application of Hume–Rothery rules – Solid Solutions
1. Would you predict more Al or Ag to dissolve in Zn?
2. More Zn or Al
in Cu?
Table on p. 135, Callister & Rethwisch 9e.
Element Atomic Crystal Electro- Valence Radius Structure nega- (nm) tivity
Cu 0.1278 FCC 1.9 +2 C 0.071 H 0.046 O 0.060 Ag 0.1445 FCC 1.9 +1 Al 0.1431 FCC 1.5 +3 Co 0.1253 HCP 1.8 +2 Cr 0.1249 BCC 1.6 +3 Fe 0.1241 BCC 1.8 +2 Ni 0.1246 FCC 1.8 +2 Pd 0.1376 FCC 2.2 +2 Zn 0.1332 HCP 1.6 +2

## Slide 15: Impurities in Solids
Specification of composition
  weight percent
m1 = mass of component 1
nm1 = number of moles of component 1
atom percent

## Slide 16: Line Defects
• are line defects,
• slip between crystal planes result when dislocations move,
• produce permanent (plastic) deformation.
Dislocations:
Schematic of Zinc (HCP):
• before deformation
• after tensile elongation
slip steps

## Slide 17: Imperfections in Solids
Linear Defects (Dislocations)
  Are one-dimensional defects around which atoms are misaligned
Edge dislocation:
  extra half-plane of atoms inserted in a crystal structure
  b perpendicular () to dislocation line
Screw dislocation:
  spiral planar ramp resulting from shear deformation
  b parallel () to dislocation line
Burger’s vector, b: measure of lattice distortion

## Slide 18: Imperfections in Solids
Edge Dislocation
Fig. 4.4, Callister & Rethwisch 9e. (Adapted from A. G. Guy, Essentials of Materials Science, McGraw-Hill Book Company, New York, NY, 1976, p. 153.)

## Slide 19: Imperfections in Solids
Screw Dislocation
Adapted from Fig. 4.5, Callister & Rethwisch 9e.
[Figure (b) from W. T. Read, Jr.,Dislocations in Crystals, McGraw-Hill Book Company, New York, NY, 1953.]
Burgers vector b
Dislocation
line
b
(a)
(b)
Screw Dislocation

## Slide 20: VMSE: Screw Dislocation
In VMSE:
  a region of crystal containing a dislocation can be rotated in 3D
  dislocation motion may be animated
Front View
Top View
VMSE Screen Shots

## Slide 21: Edge, Screw, and Mixed Dislocations
Adapted from Fig. 4.6, Callister & Rethwisch 9e. [Figure (b) from W. T. Read, Jr., Dislocations in Crystals,
McGraw-Hill Book Company, New York, NY, 1953.]
Edge
Screw
Mixed

## Slide 22: Imperfections in Solids
Dislocations are visible in electron micrographs
Fig. 4.7, Callister & Rethwisch 9e. (Courtesy of M. R. Plichta, Michigan
Technological University.)

## Slide 23: Dislocations & Crystal Structures
• Structure: close-packed
planes & directions
are preferred.
view onto two
close-packed
planes.
close-packed plane (bottom)
close-packed plane (top)
close-packed directions
• Comparison among crystal structures:
FCC: many close-packed planes/directions;
HCP: only one plane, 3 directions;
BCC: none
• Specimens that
were tensile
tested.
Mg (HCP)
Al (FCC)
tensile direction

## Slide 24: Planar Defects in Solids
One case is a twin boundary (plane)
  Essentially a reflection of atom positions across the twin plane.
Stacking faults
  For FCC metals an error in ABCABC packing sequence
  Ex: ABCABABC
Adapted from Fig. 4.10, Callister & Rethwisch 9e.

## Slide 25: Catalysts and Surface Defects
A catalyst increases the rate of a chemical reaction without being consumed
Active sites on catalysts are normally surface defects
Fig. 4.11, Callister & Rethwisch 9e.
Fig. 4.12, Callister & Rethwisch 9e.
[From W. J. Stark, L. Mädler, M. Maciejewski, S. E. Pratsinis, and A. Baiker, “Flame Synthesis of Nanocrystalline Ceria/Zirconia: Effect of Carrier Liquid,” Chem. Comm., 588–589 (2003). Reproduced by permission of The Royal Society of Chemistry.]
Single crystals of (Ce0.5Zr0.5)O2 used in an automotive catalytic converter

## Slide 26: Microscopic Examination
Crystallites (grains) and grain boundaries. Vary considerably in size. Can be quite large.
  ex: Large single crystal of quartz or diamond or Si
  ex: Aluminum light post or garbage can - see the individual grains
Crystallites (grains) can be quite small (mm or less) – necessary to observe with a microscope.

## Slide 27: Optical Microscopy
• Useful up to 2000X magnification.
• Polishing removes surface features (e.g., scratches)
• Etching changes reflectance, depending on crystal
orientation.
Micrograph of
brass (a Cu-Zn alloy)
0.75 mm
Fig. 4.14(b) & (c), Callister & Rethwisch 9e.
crystallographic planes
Courtesy of J.E. Burke, General Electric Co.

## Slide 28: Optical Microscopy
Grain boundaries...
• are imperfections,
• are more susceptible
to etching,
• may be revealed as
dark lines,
• change in crystal
orientation across
boundary.
Fig. 4.15(a) & (b), Callister & Rethwisch 9e.
[Fig. 4.15(b) is courtesy of L.C. Smith and C. Brady, the National Bureau of Standards, Washington, DC (now the National Institute of Standards and Technology, Gaithersburg, MD).]
ASTM grain
size number
N
= 2
n
-1
number of grains/in2
at 100x
magnification
Fe-Cr alloy
(b)
grain boundary
surface groove
polished surface
(a)

## Slide 29: Optical Microscopy
Polarized light
  metallographic scopes often use polarized light to increase contrast
  Also used for transparent samples such as polymers

## Slide 30: Microscopy
Optical resolution ca. 10-7 m = 0.1 μm = 100 nm
For higher resolution need higher frequency
  X-Rays? Difficult to focus.
  Electrons
    wavelengths ca. 3 pm (0.003 nm)
      (Magnification - 1,000,000X)
    Atomic resolution possible
    Electron beam focused by magnetic lenses.

## Slide 31: Scanning Tunneling Microscopy (STM)
• Atoms can be arranged and imaged!
Carbon monoxide molecules arranged on a platinum (111) surface.
Photos produced from the work of C.P. Lutz, Zeppenfeld, and D.M. Eigler. Reprinted with permission from International Business Machines Corporation, copyright 1995.
Iron atoms arranged on a copper (111) surface. These Kanji characters represent the word “atom”.

## Slide 32: Summary
• Point, Line, and Area defects exist in solids.
• The number and type of defects can be varied
and controlled (e.g., temperature controls vacancy concentration).
• Defects affect material properties (e.g., grain
boundaries control crystal slip).
• Defects may be desirable or undesirable
(e.g., dislocations may be good or bad, depending
on whether plastic deformation is desirable or not).